PARCOM RECOMMENDATION 90/1 OF 14 JUNE 1990

ON THE DEFINITION OF THE BEST AVAILABLE TECHNOLOGY FOR

SECONDARY IRON AND STEEL PLANTS

The Paris Commission agrees that as a minimum the following measures constitute the best available technology for secondary iron and steel plants:

*	Fume collection by dog-houses, local moveable hoods or total building evacuation at electric arc furnaces and converters.

*	Fabric filters or equally efficient arrestment system for dust cleaning of process gases and secondary gases from electric arc furnaces and converters.

*	Fabric filters for dust cleaning or equally efficient arrestment system at cutting, grinding and scarfing operations.

*	Regenerations of pickling baths and closing of rinse water systems.

*	Addition of hydrogen peroxide to pickling baths containing nitric acid or any equivalent measure which enables reduction of NOx to the atmosphere.

*	Sedimentation combined with filtration of waste water from continuous casting and rolling. Recirculation or re-use of the water.

*	Metal recovery from filter dust.